- Nanomaterials are materials with structural features in the range of 1–100 nm. At this scale, properties differ significantly from bulk due to quantum confinement, large surface-to-volume ratio, and modified electronic structure. Nanomaterials are synthesized in various forms: nanoparticles, nanowires, nanotubes, thin films, clusters, colloids, etc.

Two fundamental synthesis approaches exist:

2. Bottom–Up Approach

Atoms or molecules self-assemble to form nanostructures.

Common Methods

- Sol–Gel Method

- Hydrothermal synthesis

- Colloidal synthesis

- Reverse micelles

- Chemical vapor deposition

- Electrodeposition

- Template-assisted growth

Advantages

- Produces ultra-fine nanoparticles (1–20 nm)

- Good control over size/shape

- Less energy intensive

- High purity and narrow size distribution

Limitations

- Difficult for large-scale production

- Requires careful purification

- Reaction control is challenging

2.1 Sol–Gel Method

Principle

Formation of oxide networks through hydrolysis and condensation of metal alkoxides:

1st step : Hydrolysis : MOR+H2O→MOH+ROH

M = Metal atom (Si, Ti, Al, Zr, etc.), OR = Alkoxide group (e.g., –OCH₃, –OC₂H₅).

MOR = metal–alkoxide, a molecule where the metal is bonded to an alkoxy group.

Example: Si(OC₂H₅)₄ = tetraethyl orthosilicate (TEOS)

Si(OC2​H5​)4​+H2​O→Si(OC2​H5​)3​OH+C2​H5​OH  (This is the first step in forming silica (SiO₂) networks.)

2nd step : Condensation: MOH+ROM→M–O–M+ROH

This causes 1)  formation of a metal–oxygen–metal (M–O–M) network from hydroxylated metal species. The reactants are Thus the reactants are metal–hydroxide and metal–alkoxide. Both are intermediate products formed after hydrolysis. Condensation builds the 3D metal-oxide network by connecting metal atoms via oxygen bridges : M-O-M. Repeated condensation reactions link many M atoms together:  M–O–M–O–M–O–M …  This forms: clusters, chains, networks, gels.

2. Gelation:  As the network grows in 3D, the solution loses flow and transforms into a rigid gel.

3. Removal of Alcohol (ROH): Driving off ROH pushes the reaction forward and densifies the gel.

Major Steps

- Preparation of sol (stable alkoxide solution)

- Gelation via polymerization

- Aging (strengthening network)

- Drying (xerogel or aerogel formation)

- Dehydration and calcination

- Densification at high temperature

Advantages : Produces monodisperse nanoparticles, Good for thin/thick coatings, High purity, low-temperature synthesis, Can form complex shapes in gel state.

Applications: Ceramic coatings, Optical & electronic devices, Membranes (ultra-/nano-filtration), Chromatography, catalysis, biosensors

2.2 Hydrothermal Method

Principle

Chemical reactions carried out in closed autoclaves at high temperature and pressure. Water acts as both solvent and reactive species.

Steps

- Prepare aqueous precursor solution

- Heat in autoclave (≥200 °C, high pressure)

- Nucleation, growth of oxides

- Cooling, filtration, drying

Advantages: Economical, simple, Produces highly crystalline, uniform particles, Suitable for materials unstable at high temp, Very low contamination

Disadvantages: Scale-up difficult, Requires pressure vessels

Applications: Electronic ceramics, Thin film dielectrics, Oxide nanoparticles for electronics/aerospace, Semiconductor oxides

3. Top–Down Approach

Bulk solids are broken down into nanoscale structures.

Techniques

- Ball milling

- Lithography (photo-, electron-, ion-, X-ray)

- Laser ablation

- Mechanical grinding

- Aerosol spray, gas-phase condensation

Advantages : Simple and industrially scalable,Cost-effective,Produces uniform chemical composition

Disadvantages : Surface defects and roughness, size non-uniformity, Equipment dependency

3.1 Ball Milling (Mechanical Alloying)

High-energy balls collide with powder to reduce particle size (down to 2–20 nm).

Advantages: Large-scale production, Inexpensive and simple, Suitable for alloys, oxides, ceramics

Limitations : Irregular particle shape, Contamination, Crystal defects introduced

Applications

- Metal/oxide nanocrystals, Intermetallics (Ni–Al, etc.), Novel building materials

3.2 Lithography

Patterning at micro/nanoscale by selective removal/exposure.

Steps involved in Photo-Lithography are

- Substrate cleaning

- Resist coating

- Exposure (UV, e-beam, ion)

- Development

- Etching/deposition

- Lift-off

Types

- Photolithography

- Electron-beam lithography

- X-ray lithography

- Nanoimprint lithography

Applications : Semiconductor ICs, MEMS/NEMS, Sensors, waveguides, Quantum devices

3.3 Laser Ablation (Pulsed Laser Deposition)

High-energy pulsed laser vaporizes the target; vapor condenses on substrate forming thin films.

Advantages : Ultrapure films, Precise control of film composition, Applicable to most inorganic materials

Disadvantages : Slow deposition rate, Expensive equipment, Line-of-sight limitation

4. Nanoscale Semiconductors & Quantum Dots

Quantum Confinement

When particle dimension becomes comparable to the electron de Broglie wavelength:

- Energy levels become discrete

- Bandgap increases as size decreases

Density of States (DOS) Summary: 3D bulk: continuous, 2D films: step-like, 1D wires: spikes, 0D quantum dots: discrete levels (“artificial atoms”)

Optical Properties

- Smaller particles → blue shift (shorter wavelength)

- Larger particles → red shift

- Strong fluorescence due to discrete states

Electrical Properties

- Coulomb blockade in quantum dots

- Lower carrier mobility

- Dominant tunneling effects

Applications

- QLED displays

- Bio-imaging probes

- Quantum computing (spin qubits)

- Solar cells and lasers

- Chemical/optical sensors

5. Summary

Key Ideas

- Nanomaterials exhibit unique properties due to quantum confinement and large surface area.

- Bottom-up methods assemble atoms into nanostructures; top-down methods break bulk into nanoscale.

- Sol-gel and hydrothermal methods are highly versatile for preparing oxides and ceramics.

- Ball milling, lithography, and laser ablation are critical industrial tools.

- Quantum dots behave like artificial atoms with size-tunable optical and electrical properties.

Why This Matters for Mechanical Engineers

- Nanostructured materials enhance strength, wear resistance, thermal properties.

- Nanoscale coatings improve corrosion resistance and conductivity.

- Quantum-confined materials are used in sensors, actuators, MEMS/NEMS systems.

- Understanding synthesis helps in selecting materials for advanced manufacturing.